## Slide 1: SNF RRAM Standard Process Flow and Characterization of Lesker-2 TiN
Project Members: Akash Levy, Jung-Soo Ko
Staff Mentors: Michelle Rincon, Vijay Narasimhan, J Provine, Usha Raghuram
ENGR241 Week 5 Updates

## Slide 2: Aim & Goals
  Test and characterize ALD RRAM devices
  Develop TiN recipe on new Lesker with low oxygen contamination
  Compare TiN properties (composition, resistivity, topography)
  Make electrical/imaging data and test structure layouts available to SNF
  Make SOPs for RRAM stacks and report TiN findings
Process Flow Development
Parameter Optimization
Comprehensive Documentation
SNF Database

## Slide 3: Progress Updates: Fabrication
  Clean and grow SiO2 for isolation
  Sputter 30nm TiN (Sharpie for step)
    AJA (non-SNF)
    Lesker-1 (SNF)
    Lesker-2 (SNF)
  AJA Characterization
    XPS
    Prometrix
    AFM
    Alphastep
    Auger
  Lesker-1 Characterization
    XPS
    Prometrix
    AFM
    Alphastep
    Auger
  Lesker-2 Characterization
Si
SiO2
TiN
Update: Lesker-2 training starting soon!
Underlined is planned to be done by next checkpoint

## Slide 4: TiN Film Comparison
AJA
Lesker-1

## Slide 5: Literature Review on TiN Sputtering
  TiN films absorb a high concentration of contaminants including hydrogen, carbon, and oxygen when they are exposed to air after deposition
  With the target–substrate distance set to 88 mm the contaminant levels increase from ∼0.1% to ∼10% as the pressure is increased from 2 to 9 mTorr
  The contaminant concentrations also correlate with in-plane distance from the center of the substrate and increase by roughly two orders of magnitude as the target–substrate distance is increased from 88 to 266 mm
  Contaminants strongly influence properties of TiN thin films
  Resistivity of stoichiometric films increases by around a factor of 5 as the oxygen content increases from 0.1% to 11%
  Energy of the sputtered TiN particles plays crucial role in determining the film properties
  Important to precisely control the energy of these particles to obtain high-quality TiN
Ohya, S., B. Chiaro, A. Megrant, C. Neill, R. Barends, Y. Chen, J. Kelly et al. "Room temperature deposition of sputtered TiN films for superconducting coplanar waveguide resonators." Superconductor Science and Technology 27, no. 1 (2013): 015009.

## Slide 6: TiN Properties
 | AJA: A1 | Lesker-1: X1 | Lesker-1: X2 | Lesker-1: X3 | Lesker-1: X4 | Lesker-1: X5
Target | Ti | TiN | TiN | TiN | Ti | TiN
Base Pressure | ~1e-7 Torr | ~1e-6 Torr | ~1e-6 Torr | ~1e-7 Torr (?) | ~1e-7 Torr (?) | ~1e-7 Torr
RF Power | 200W | 150W | 200W | 200W | 200W | 200W
Gettering/Chamber Conditioning | 2 min TiN | 2 min TiN | 5 min Ti, 5 min TiN | 5 min Ti, 5 min TiN | 5 min Ti, 5 min TiN | 10 min Ti, 5 min TiN
Wafer Bias | 100V | 100V | 100V | 100V | 100V | 100V
Ar/N Flow | 30/3 sccm | 50/5 sccm | 30/3 sccm | 30/0 sccm | 30/3 sccm | 30/3 sccm
Pressure | 2.15 mTorr | 5 mTorr | 3 mTorr (5.5) | 2 mTorr | 2 mTorr | 2 mTorr
Sheet Resistance | 15.650 Ω/□ | ? | ? |  |  | 
Resistivity | ? | ? | ? |  |  | 
Uniformity/Color | Excellent | Bad | Good |  |  | 
Thickness/Time | ?nm/1800s | ?nm/1800s | ?nm/900s |  |  | ?nm/1800s
Roughness | 0.67nm | ? | ? |  |  | 
Composition (Ti:N:O) | 46:51:3 | ? | ? |  |  | 

## Slide 7: Progress Updates
  RCA clean wafer
  Grow 50nm SiO2 with thermco4 (20 min. of 900C wet growth)
  Deposit 10nm Ti with AJA (skipped)
  Deposit 30nm Pt with AJA
  Deposit 100nm SiO2 with AJA
  Woollam to check oxide thickness (834Å)
  Photolithography (1)
    YES Oven for 30 mins
    SVG Coat 2 with 1µm Shipley 3612 resist, 2mm EBR, skip prime step
    Expose with Heidelberg (use defoc: -2, dose: 70/80 for Heidelberg1/2, 350nm)
    SVG Develop (1µm 3612 dev) w/post-exposure bake and inspect
  PT-Ox: Oxide_ER_Test, 1 min
  Resist ashing: Gasonics recipe 003 (1)
  Metal cleaning on wbflexcorr (1)
    SRS-100 for stripping photoresist from metal wafers, 60C
    PRS-1000 for final metal clean before deposition or furnace step, 40C
  Alphastep to check etching
  Fiji1 thermal HfO2: 100 cyc. std. recipe
  Woollam to check oxide thickness
  TiN deposition 30nm
  Photolithography (2)
  PT-MTL: still need details
  Microscope to check etching
  Resist ashing: Gasonics recipe 003 (2)
  Metal cleaning on wbflexcorr (2)
  Electrical testing
Underlined is planned to be done by next checkpoint
Notes: Dose: 70, defoc: -2 on Heidelberg-2
Dose: 80ish, defoc: -2 on Heidelberg-1

## Slide 8: Thank you!
Questions?

## Slide 9: AFM Roughness Measurements: AJA
Roughness: 1.02nm SiO2
Roughness: 1.22nm TiN
0.67nm independent

## Slide 10: AJA TiN Sputter Recipe: Reactive Sputtering
  Target: Ti
  RF Power: 200W
    150W also ok; different dep rates
  Wafer Bias: 100V
    DC bias 92-94V on AJA in practice
  Ar Flow: 30 sccm
  N Flow: 3 sccm
    Unit conversion means that this is written as 30 on AJA somehow
  Set Pressure: 2.15 mTorr
    1.8-1.9 mTorr on AJA in practice
  Recipe:
  Load sample and wait for 1e-7 base chamber pressure
  Plasma on another target (conductive) e.g. Al, GeTe
    Eases plasma ignition for TiN target
  Plasma on Ti target
    Bias on other target off
  20s ramp-up of Ti target RF power
  2 minutes pre-sputtering of Ti target (shutter closed, no wafer bias)
  20s ramp-up of wafer bias
  Open shutter and deposit for X seconds
  Close shutter
  20s ramp-down of Ti target RF power