## Slide 1: SNF RRAM Standard Process Flow and Characterization of Lesker-2 TiN
Project Members: Akash Levy, Jung-Soo Ko
Staff Mentors: Michelle Rincon, Vijay Narasimhan, J Provine, Usha Raghuram
ENGR241 Week 9 Updates

## Slide 2: Aim & Goals
  Test and characterize ALD RRAM devices
  Develop TiN recipe on new Lesker with low oxygen contamination
  Compare TiN properties (composition, resistivity, topography)
  Make electrical/imaging data and test structure layouts available to SNF
  Make SOPs for RRAM stacks and report TiN findings
Process Flow Development
Parameter Optimization
Comprehensive Documentation
SNF Database

## Slide 3: Progress Updates: Fabrication
  Clean and grow SiO2 for isolation
  Sputter 30nm TiN (Sharpie liftoff for step)
    AJA (non-SNF)
    Lesker-1 (SNF)
    Lesker-2 (SNF)
  Characterization
    XPS composition
    Prometrix resistivity
    AFM step height/surface roughness
    Alphastep
  Lesker 2: giving low-resistivity TiN finally 
Si
SiO2
TiN

## Slide 4: Lesker-2 TiN: good chamber pressure = low resistivity

## Slide 5: TiN Properties
 | AJA: A1 | Lesker-1: X2 | Lesker-1: X3 | Lesker-1: X4 | Lesker-2: Y1 | Lesker-2: Y2 | L-2: Y3 | L-2: Y4 | L-2: Y5
Target/Wafer | Ti/Si+SiO2 | TiN/Si+SiO2 | TiN/Si+SiO2 | TiN/Si+SiO2 | TiN/Si+SiO2 | TiN/Si+SiO2 | TiN/glass | TiN/glass | TiN/glass
Base Pressure | ~1e-7 Torr | ~1e-6 Torr | ~1e-6 Torr (?) | ~1e-6 Torr | ~1e-7 Torr | ~4e-9 Torr | ~1e-8 Torr | ~1e-8 Torr | ~1e-8 Torr
RF Power | 200W | 200W | 200W | 200W | 200W | 200W | 100W | 150W | 250W
Gettering/ Chamber | 2 min TiN ↑ | 5 min Ti pre, 5 min TiN ↑ | 10 min Ti pre, 5 min TiN ↑ | 5 min Ti pre, 5 min TiN ↑ | 5 min TiN pre, 5 min TiN ↑ | 30 min TiN pre, 5 min TiN ↑ | See prev. | See prev. | See prev.
Wafer Bias | 100V | 100V | 100V | 100V | 100V | 100V | 100V | 100V | 100V
Ar/N Flow | 30/3 sccm ↓ | 30/3 sccm ↓ | 30/3 sccm ↓ | 30/0 sccm ↓ | 11.5/0 sccm ↑ | 11.6/0 sccm ↑ | See prev. | See prev. | See prev.
Pressure | 2.15 mTorr | 30->3 mTorr | 20->2 mTorr | 20->2 mTorr | 15->2 mTorr | 15->2 mTorr | See prev. | See prev. | See prev.
Sheet Resistance | 15.650 Ω/□ | 2428.0 Ω/□ | 304.8 Ω/□ | 129.9 Ω/□ | 121.2 Ω/□ | 54.4 Ω/□ |  |  | 
Resistivity | 67.25 uΩ cm | 6313 uΩ cm | 927 uΩ cm | 519.6 uΩ cm | ? | ? |  |  | 
Uniformity/Color | Excellent | Okay | Good | Good | Good | Good |  |  | 
Thickness/Time | 43nm/1800s | 26nm/900s | 30.4nm/1800s | 40nm/1800s | ?/1800s | ?/1800s | ?/1800s | ?/1800s | ?/1800s
Roughness | 0.67nm | ? | ? | ? | ? | ? | ? | ? | ?
Composition (Ti:N:O) | 46:51:3 | 38:39:23 | 43:43:14 | 43:43:14 | ? | ? | ? | ? | ?

## Slide 6: RRAM Process Flow Outline
Si
Si
Pt
SiO2
Start with Si wafer
Standard RCA Clean
Deposit 10nm Ti, 30nm Pt (AJA),
150nm SiO2 (ccp-dep)
Si
Pt
SiO2
Pattern trenches (PT-Ox)
Post-metal clean
SiO2
Si
Pt
SiO2
SiO2
HfO2
Deposit 10nm HfO2 (Fiji)
Si
Pt
SiO2
SiO2
HfO2
TiN
Sputter 30nm TiN
Si
Pt
SiO2
SiO2
HfO2
TiN
Pattern top electrodes (PT-MTL)
Post-metal clean
Active device area
(Not drawn to scale)

## Slide 7: Progress Updates: S1
  RCA clean wafer
  Grow 50nm SiO2 with thermco4 (20 min. of 900C wet growth)
  Deposit 10nm Ti on AJA (0.5Å/s)
  Deposit 30nm Pt on AJA (1Å/s)
  Deposit 150nm SiO2 with ccp-dep (SiO350-0, SiOx1 350C, 2.5 min)
  Woollam to check SiO2 thickness
    Measure 55-75 degrees, use n-k fit for SiO2
    S1: 2320Å, R1: 1504Å
  Photolithography (1)
    YES Oven default recipe
    SVG Coat 2 with 1µm Shipley 3612 resist, 2mm EBR, skip vapor prime step
    Expose with Heidelberg (use defoc: -2, dose: 70/80 for Heidelberg1/2, 350nm laser src)
    SVG Develop (1µm 3612 dev) w/post-exposure bake and inspect
  PT-Ox: Ox_ER_Test, 210 sec.
  Resist ashing: Matrix default recipe
  Metal cleaning on wbflexcorr (1)
    SRS-100 for stripping photoresist from metal wafers, 60C, 20 min
    PRS-1000 for final metal clean before deposition, 40C, 10 min
  Alphastep to check etching
    Matched Woollam extremely well
  Fiji1 thermal HfO2: 50 cyc. condition,100 cyc. @ 200C
  Woollam to check HfO2 thickness
    Measure 55-75 degrees, use n-k for SiO2 from before thickness and n-k from before
    S1: 182Å, R1: 229Å, R2: 233Å, R3: 130Å
    Strangely high deposition rate (multi-cycle/step?)
  TiN deposition 30nm
  Photolithography (2)
  Microscope to ensure patterns are aligned
  PT-MTL: Al-HiPRSel-Usha, 30s
    Should etch through all of TiN and some oxide
  Microscope to ensure TiN is patterned correctly
  Metal cleaning on wbflexcorr (2)
  Electrical testing
Notes: Dose: 70, defoc: -2 on Heidelberg-2
Dose: 80ish, defoc: -2 on Heidelberg-1

## Slide 8: Progress Updates: R1
  RCA clean wafer
  Grow 50nm SiO2 with thermco4 (20 min. of 900C wet growth)
  Deposit 10nm Ti on AJA (0.5Å/s)
  Deposit 30nm Pt on AJA (1Å/s)
  Deposit 150nm SiO2 with ccp-dep (SiO350-0, SiOx1 350C, 2.5 min)
  Woollam to check SiO2 thickness
    Measure 55-75 degrees, use n-k fit for SiO2
    S1: 2320Å, R1: 1504Å
  Photolithography (1)
    YES Oven default recipe
    SVG Coat 2 with 1µm Shipley 3612 resist, 2mm EBR, skip vapor prime step
    Expose with Heidelberg (use defoc: -2, dose: 70/80 for Heidelberg1/2, 350nm laser src)
    SVG Develop (1µm 3612 dev) w/post-exposure bake and inspect
  PT-Ox: Ox_ER_Test, 210 sec.
  Resist ashing: Matrix default recipe
  Metal cleaning on wbflexcorr (1)
    SRS-100 for stripping photoresist from metal wafers, 60C, 15 min
    PRS-1000 for final metal clean before deposition, 40C, 10 min
  Alphastep to check etching
    Matched Woollam extremely well
  Fiji1 thermal HfO2: 50 cyc. condition,100 cyc. @ 200C
  Woollam to check HfO2 thickness
    Measure 55-75 degrees, use n-k for SiO2 from before thickness and n-k from before
    S1: 182Å, R1: 229Å, R2: 233Å, R3: 130Å
    Strangely high deposition rate (multi-cycle/step?)
  TiN deposition 30nm
  Photolithography (2)
  Microscope to ensure patterns are aligned
  PT-MTL: Al-HiPRSel-Usha, 30s
    Should etch through all of TiN and some oxide
  Microscope to ensure TiN is patterned correctly
  Metal cleaning on wbflexcorr (2)
  Electrical testing
Notes: Dose: 70, defoc: -2 on Heidelberg-2
Dose: 80ish, defoc: -2 on Heidelberg-1

## Slide 9: Sample with AJA TiN: weird diffraction effect pre-pattern

## Slide 10: S1 Sample Images (pre-final clean)
  This is the area of the sample outside of the contact patterning area
  Resistivity is very high in this area
  Was PR not fully removed?
    Worse alternative: is TiN resistivity high?
  Scratching a bit with probes leads to low resistivity
  Pinholes are probably resist residues

## Slide 11: S1 Sample Images (pre-final clean)
  In some portions of the wafer, the pinholes do not seem to preferentially target the trenches  (TOP, 1um trenches)
  In other areas, the pinholes seem to almost always be in the cell active area  (BOTTOM, 2um trenches)
  Probing any two spots on yellow area (no contact) has low resistivity (in 10s of ohms) so seems that we have over-etched through SiO2
  So last patterning step is not necessary?

## Slide 12: S1 Sample Images (pre-final clean)
Pretty good images
Pinholes missed 

## Slide 13: S1 Sample Images (intermediate steps)
  TOP: post-develop
  BOTTOM: post-etch

## Slide 14: S1 Sample Image (final)
  Things that went wrong with S1:
    TiN film did not look right
    Overetch (85s) with PT-MTL
      Could have eaten through all of 1um 3612 PR! Etch rate can be >7000 um/min
    Possible oxidation of TiN with final matrix plasma clean step
  Devices did not work at all
    Did not even show hard breakdown
  Unclear if contacts are metallic or just SiO2

## Slide 15: R1: RRAM that FORMs and RESETs 
  Fixes to process flow:
    Lesker-2 TiN was used
      Color looked similar to blanket depositions on Si
      Resistivity confirmed to be relatively low
    60s etch in PT-MTL:
      Photoresist appears to still be present 
      Uncovered areas expose Pt
    No matrix ash: straight to SRS-100/PRS-1000
  Early result from 3 PM today:
    (40 um x 40 um) devices work!
    Can FORM, RESET great
    SET is having issues: over-SET

## Slide 16: Final Week
  Characterizing R1 devices:
    Tuning test setup for SET to prevent over-SET problem
    Slow sweep and compliance current adjustment
  Fabricating/characterizing TiN devices that Graham though would be useful
    3 more blanket samples to deposit (on glass wafers)
      Different RF powers
        100W, 150W, 200W (already done), 250W
    Prometrix sheet resistance on Lesker-2 TiN samples
    XPS on Lesker-2 TiN samples
    Step height on Lesker-2 TiN samples for deposition rate/resistivity
    Surface roughness on all TiN samples
  R2 and R3 are in the pipeline and can be completed
    What parameters to use? Just get variability?

## Slide 17: Thank you!
Questions?

## Slide 18: AJA TiN Sputter Recipe: Reactive Sputtering
  Target: Ti
  RF Power: 200W
    150W also ok; different dep rates
  Wafer Bias: 100V
    DC bias 92-94V on AJA in practice
  Ar Flow: 30 sccm
  N Flow: 3 sccm
    Unit conversion means that this is written as 30 on AJA somehow
  Set Pressure: 2.15 mTorr
    1.8-1.9 mTorr on AJA in practice
  Recipe:
  Load sample and wait for 1e-7 base chamber pressure
  Plasma on another target (conductive) e.g. Al, GeTe
    Eases plasma ignition for TiN target
  Plasma on Ti target
    Bias on other target off
  20s ramp-up of Ti target RF power
  2 minutes pre-sputtering of Ti target (shutter closed, no wafer bias)
  20s ramp-up of wafer bias
  Open shutter and deposit for X seconds
  Close shutter
  20s ramp-down of Ti target RF power

## Slide 19: Literature Review on TiN Sputtering
  TiN films absorb a high concentration of contaminants including hydrogen, carbon, and oxygen when they are exposed to air after deposition
  With the target–substrate distance set to 88 mm the contaminant levels increase from ∼0.1% to ∼10% as the pressure is increased from 2 to 9 mTorr
  The contaminant concentrations also correlate with in-plane distance from the center of the substrate and increase by roughly two orders of magnitude as the target–substrate distance is increased from 88 to 266 mm
  Contaminants strongly influence properties of TiN thin films
  Resistivity of stoichiometric films increases by around a factor of 5 as the oxygen content increases from 0.1% to 11%
  Energy of the sputtered TiN particles plays crucial role in determining the film properties
  Important to precisely control the energy of these particles to obtain high-quality TiN
Ohya, S., B. Chiaro, A. Megrant, C. Neill, R. Barends, Y. Chen, J. Kelly et al. "Room temperature deposition of sputtered TiN films for superconducting coplanar waveguide resonators." Superconductor Science and Technology 27, no. 1 (2013): 015009.