## Slide 1: SNF RRAM Standard Process Flow and Characterization of Lesker-2 TiN
Project Members: Akash Levy, Jung-Soo Ko
Staff Mentors: Michelle Rincon, Vijay Narasimhan, J Provine, Usha Raghuram
ENGR241 Week 3 Updates

## Slide 2: Aim & Goals
  Test and characterize ALD RRAM devices
  Develop TiN recipe on new Lesker with low oxygen contamination
  Compare TiN properties (composition, resistivity, topography)
  Make electrical/imaging data and test structure layouts available to SNF
  Make SOPs for RRAM stacks and report TiN findings
Process Flow Development
Parameter Optimization
Comprehensive Documentation
SNF Database

## Slide 3: Tool Training Update
  Finished training on:
  Heidelberg
  SVG Coat
  SVG Develop
  Thermco
  Coming up:
  XPS qualification (Thursday)
  Almost done with training on tools! 
  Need refresher on PT-Ox/PT-MTL though…

## Slide 4: TiN Sample Preparation & Characterization
Si
Si
SiO2
Start with Si wafer
Standard RCA Clean
Dry grow 100nm SiO2
(thermco)
Si
SiO2
Sputter 30nm TiN
TiN
(Not drawn to scale)
AFM Surface Roughness
Compare 3 sputtering tools: Lesker-1 (SNF), Lesker-2 (SNF), AJA (non-SNF)
AFM/Woollam
Step Height
Prometrix Resistivity
XPS/Auger Composition
Measure 3-4x throughout quarter to quantify oxidation over time

## Slide 5: Progress Updates: Fabrication
  RCA clean wafer
  Woollam to measure native oxide thickness (11.2Å)
  Dry oxide growth for 1hr in thermco4 @ 1100℃ (~100nm)
  Woollam to confirm final oxide thickness (~1062.54Å, ~1052.91Å)
    Exact thickness is not important, just there to insulate TiN from Si
    Good quality oxide is important to get accurate TiN surface roughness
  Sputter 30nm TiN (Kapton tape for step)
    AJA (non-SNF)
    Lesker-1 (SNF)
    Lesker-2 (SNF)
  Characterization
Lesker TiN target
Si
SiO2
TiN
Update: Lesker-2 expected to go live in early Feb.

## Slide 6: RRAM Process Flow Outline
Si
Si
Pt
SiO2
Start with Si wafer
Standard RCA Clean
Deposit 30nm Pt,
100nm SiO2 (AJA)
Si
Pt
SiO2
Pattern trenches (PT-Ox)
Clean sidewalls of trenches
SiO2
Si
Pt
SiO2
SiO2
HfO2
Deposit 10nm HfO2 (Fiji)
Si
Pt
SiO2
SiO2
HfO2
TiN
Sputter 30nm TiN
Si
Pt
SiO2
SiO2
HfO2
TiN
Pattern top electrodes
(PT-MTL)
Active device area
(Not drawn to scale)

## Slide 7: Process Flow Parameters
  Resistive switching material (metal oxide): hafnia, alumina, zirconia, tantala, titania
  Seed layer: none, 1nm, 2nm
  Dimensions:
    TiN electrode thickness: 5nm, 10nm, 20nm, 30nm, 50nm
    Resistive switching layer thickness: 2nm, 5nm, 8nm, 10nm, 15nm
    Device size: ﻿{1, 2, 3, 4, 5, 8, 10, 20, 40, 50} um
  RS oxide growth temperature: 200C, 250C, 300C
  Anneal temperature: none, 300C, 400C
  Metal oxide ALD method: plasma, thermal
    Theory: thermal ALD will work better since plasma is known to cause interface traps and can also potentially sputter BE metal
  TiN deposition method: ALD vs. sputtered
    Theory: ALD TiN will not work because of oxygen contamination
    Optimize (sputter): substrate bias, temperature, sputtering gases, etc.
  Top contact: Au, Ag, TiN only

## Slide 8: Progress Updates
  Finalized most of the process flow details and single device array layouts!
  RCA clean wafer
  Deposit 10nm Ti with AJA (skipped)
  Deposit 30nm Pt with AJA
  Deposit 100nm SiO2 with AJA
  Woollam to check oxide thickness (834Å, 21.33 MSE)
  Photolithography
    YES Oven for 30 mins
    SVG Coat 2 with 1µm Shipley 3612 resist, 2mm EBR, skip prime step
    Expose with Heidelberg: look at previous runs, logbook, exposure charts next to tool (dose: 80, defocus: ±2?)
    SVG Develop (1µm 3612 dev) w/post-exposure bake and inspect
  PT-Ox: 1700 Å/min (look at monitor log), so etch for ~45 seconds: jkPRmask OxSTD, seO2Clean-1
  Matrix for resist ashing: use defaults (Strip.rcp 120s) and inspect to see if resist is removed
  Fiji1 thermal HfO2: 100 cycles standard recipe
  Woollam to check oxide thickness
  TiN deposition 30nm
  Photolithography (see previous steps)
  PT-MTL: still need details
  Matrix for resist ashing: use default recipe (Strip.rcp 120s) and inspect to see if resist is removed
    (Should we worry about TiN oxidation from oxygen plasma?)
Just finished litho training!
Hoping to get here by next Tuesday

## Slide 9: Layout Generator

## Slide 10: Layout Generator
Finalized layout: alignment marks, tiling, centering about origin to make Heidelberg usage easier
Design dimensions: about 4cm x 4cm, (20x3 array) x (4x2 grid) devices per size with 10 device sizes
Trench Layer
Top Electrode Layer

## Slide 11: Characterization for this week
2 samples
AFM step height
-surface roughness (sio2, tin)
-step height (tape)
(will do ellipsometry for comparison)
Auger
-composition
Prometrix training  Ask marc for help
(eventually get trained on it)

## Slide 12: Thank you!
Questions?