## Slide 1: SNF RRAM Standard Process Flow and Characterization of Lesker-2 TiN
Project Members: Akash Levy, Jung-Soo Ko
Staff Mentors: Michelle Rincon, Vijay Narasimhan, J Provine, Usha Raghuram
ENGR241 Final Presentation

## Slide 2: Aim & Goals
  Test and characterize ALD RRAM devices
  Develop TiN recipe on new Lesker with low oxygen contamination
  Compare TiN properties (composition, resistivity, topography)
  Make electrical/imaging data and test structure layouts available to SNF
  Make SOPs for RRAM stacks and report TiN findings
Process Flow Development
Parameter Optimization
Comprehensive Documentation
SNF Database

## Slide 3: TiN Sample Preparation & Characterization
Si
Si
SiO2
Start with Si wafer
Standard RCA Clean
Dry grow 100nm SiO2
(thermco)
Si
SiO2
Sputter 30nm TiN
TiN
(Not drawn to scale)
AFM Surface Roughness
Compare 3 sputtering tools: Lesker-1 (SNF), Lesker-2 (SNF), AJA (non-SNF)
AFM Step Height
Prometrix Resistivity
XPS Composition + Milling

## Slide 4: Literature Review on TiN Sputtering
  TiN films absorb a high concentration of contaminants including hydrogen, carbon, and oxygen when they are exposed to air after deposition
  With the target–substrate distance set to 88 mm the contaminant levels increase from ∼0.1% to ∼10% as the pressure is increased from 2 to 9 mTorr
  The contaminant concentrations also correlate with in-plane distance from the center of the substrate and increase by roughly two orders of magnitude as the target–substrate distance is increased from 88 to 266 mm
  Contaminants strongly influence properties of TiN thin films
  Resistivity of stoichiometric films increases by around a factor of 5 as the oxygen content increases from 0.1% to 11%
  Energy of the sputtered TiN particles plays crucial role in determining the film properties
  Important to precisely control the energy of these particles to obtain high-quality TiN
Ohya, S., B. Chiaro, A. Megrant, C. Neill, R. Barends, Y. Chen, J. Kelly et al. "Room temperature deposition of sputtered TiN films for superconducting coplanar waveguide resonators." Superconductor Science and Technology 27, no. 1 (2013): 015009.

## Slide 5: AJA TiN Sputter Recipe: Reactive Sputtering
  Target: Ti
  RF Power: 200W
    150W also ok; different dep rates
  Wafer Bias: 100V
    DC bias 92-94V on AJA in practice
  Ar Flow: 30 sccm
  N Flow: 3 sccm
    Unit conversion means that this is written as 30 on AJA somehow
  Set Pressure: 2.15 mTorr
    1.8-1.9 mTorr on AJA in practice
  Recipe:
  Load sample and wait for 1e-7 base chamber pressure
  Plasma on another target (conductive) e.g. Al, GeTe
    Eases plasma ignition for TiN target
  Plasma on Ti target
    Bias on other target off
  20s ramp-up of Ti target RF power
  2 minutes pre-sputtering of Ti target (shutter closed, no wafer bias)
  20s ramp-up of wafer bias
  Open shutter and deposit for X seconds
  Close shutter
  20s ramp-down of Ti target RF power

## Slide 6: TiN Properties
 | AJA: A1 | Lesker-1: X2 | Lesker-1: X3 | Lesker-1: X4 | Lesker-2: Y1 | Lesker-2: Y2 | Lesker-2: Y3 | Lesker-2: Y4
Target/Wafer | Ti/Si+SiO2 | TiN/Si+SiO2 | TiN/Si+SiO2 | TiN/Si+SiO2 | TiN/Si+SiO2 | TiN/Si+SiO2 | TiN/glass | TiN/glass
Base Pressure | ~1e-7 Torr | ~1e-6 Torr | ~3e-6 Torr | ~1e-6 Torr | ~1e-7 Torr | ~4e-9 Torr | ~1e-8 Torr | ~2e-8 Torr
RF Power | 200W | 200W | 200W | 200W | 200W | 200W | 250W | 150W
Gettering/ Chamber | 2 min TiN ↑ | 5 min Ti pre, 5 min TiN ↑ | 10 min Ti pre, 5 min TiN ↑ | 5 min Ti pre, 5 min TiN ↑ | 5 min TiN pre, 5 min TiN ↑ | 30 min TiN pre, 5 min TiN ↑ | 30 min TiN pre, 5 min TiN ↑ | 30 min TiN pre, 5 min TiN ↑
Wafer Bias | 100V | 100V | 100V | 100V | 100V | 100V | 100V | 100V
Ar/N Flow | 30/3 sccm ↓ | 30/3 sccm ↓ | 30/3 sccm ↓ | 30/0 sccm ↓ | 11.5/0 sccm ↑ | 11.6/0 sccm ↑ | 11.5/0 sccm ↑ | 11.5/0 sccm ↑
Pressure | 2.15 mTorr | 30->3 mTorr | 20->2 mTorr | 20->2 mTorr | 15->5->2 mTorr | 15->5->2 mTorr | 15->5->2 mTorr | 15->5->2 mTorr
Sheet Resistance | 15.650 Ω/□ | 2428.0 Ω/□ | 304.8 Ω/□ | 129.9 Ω/□ | 121.2 Ω/□ | 54.4 Ω/□ | 43.5 Ω/□ | 110.2 Ω/□
Resistivity | 67.25 uΩ cm | 6313 uΩ cm | 927 uΩ cm | 519.6 uΩ cm | 969.6 uΩ cm | 217.6 uΩ cm | 326.2 uΩ cm | 639.2 uΩ cm
Uniformity/Color | Excellent | Not Good | Okay | Okay | Okay | Okay | Okay | Okay
Thickness/Time | 43nm/1800s | 26nm/900s | 30nm/1800s | 40nm/1800s | 80nm/1800s | 40nm/1800s | 75nm/1800s | 58nm/1800s
Roughness | 0.67nm | 1.79nm | 1.66nm | 1.37nm | 0.86nm | 1.28nm | ? | ?
Composition (Ti:N:O) | 47:52:1 | 38:39:23 | 43:43:14 | 43:43:14 | 46:41:13 | 47:40:13 | 45:42:13 | 48:45:7
Seems to have different deposition rates for glass and Si
Probably difference in effect of wafer bias!

## Slide 7: RRAM Process Flow Outline
Si
Si
Pt
SiO2
Start with Si wafer
Standard RCA Clean
Deposit 10nm Ti, 30nm Pt (AJA),
150nm SiO2 (ccp-dep)
Si
Pt
SiO2
Pattern trenches (PT-Ox)
Post-metal clean
SiO2
Si
Pt
SiO2
SiO2
HfO2
Deposit 10nm HfO2 (Fiji)
Si
Pt
SiO2
SiO2
HfO2
TiN
Sputter 30nm TiN
Si
Pt
SiO2
SiO2
HfO2
TiN
Pattern top electrodes (PT-MTL)
Post-metal clean
Active device area
(Not drawn to scale)

## Slide 8: Layout Generator

## Slide 9: Layout Generator
Finalized layout: alignment marks, tiling, centering about origin to make Heidelberg usage easier
Design dimensions: about 4cm x 4cm, (20x3 array) x (4x2 grid) devices per size with 10 device sizes
Trench Layer
Top Electrode Layer

## Slide 10: R1: RRAM that FORMs and RESETs 
  Fixes to process flow:
    Lesker-2 TiN was used
      Color looked similar to blanket depositions on Si
      Resistivity confirmed to be relatively low
    60s etch in PT-MTL:
      Photoresist appears to still be present 
      Uncovered areas expose Pt
    No matrix ash: straight to SRS-100/PRS-1000
  Results so far:
    (40 um x 40 um) devices work!
    Can FORM, RESET great
    SET is having issues: over-SET

## Slide 11: Preliminary RRAM Characteristics (40um x 40um)
FORMING
RESET

## Slide 12: Final Week
  Characterizing R1 devices:
    Tuning test setup for SET to prevent over-SET problem
    Slow sweep and compliance current adjustment
  Fabricating/characterizing TiN devices that Graham though would be useful
    XPS on Lesker-2 TiN samples
    Surface roughness on all TiN samples
  Community service project goals:
    Characterize TiN deposition rate
    Compare to reactive sputtering with Ti target
    RRAM sample optimization and statistical analysis

## Slide 13: Challenges of ALD on 2D
C. Park, H. Kim et al., RSC Adv., 2017.
C. Wirtz et al., RSC, 2015.
Challenges with ALD on 2D materials:
  Lack of dangling bonds
   No nucleation sites
Difficult to make top gated structure!
Surface functionalization required to create nucleation sites!
Precursor
Notes: Instead of using TMA, use precursor
Edit the right figures

## Slide 14: Top Gating 2D FET: Process Flow
MoS2
SiO2
P++ Si
Au
Au
Au
ALD oxide
Ti
Seed
Contact Pads for Probing
Metal-MoS2 Contact
Channel Definition
Metal Gate Deposition
Etching through Oxide for Probing
ALD oxide
Seed
ALD oxide
Seed

## Slide 15: Thank you!
Questions?