## Slide 1: SNF RRAM Standard Process Flow and Characterization of Lesker-2 TiN
Project Members: Akash Levy, Jung-Soo Ko
Staff Mentors: Michelle Rincon, Vijay Narasimhan, J Provine, Usha Raghuram
ENGR241 Week 4 Updates

## Slide 2: Aim & Goals
  Test and characterize ALD RRAM devices
  Develop TiN recipe on new Lesker with low oxygen contamination
  Compare TiN properties (composition, resistivity, topography)
  Make electrical/imaging data and test structure layouts available to SNF
  Make SOPs for RRAM stacks and report TiN findings
Process Flow Development
Parameter Optimization
Comprehensive Documentation
SNF Database

## Slide 3: Tool Training Update
  XPS qualification
  Refresher on PT-Ox/PT-MTL
  Wet bench: wbflexcorr
    For sidewall/oxide/resist cleaning process
  Need a bit more characterization:
  Prometrix
  Nanospec
  P2

## Slide 4: TiN Sample Preparation & Characterization
Si
Si
SiO2
Start with Si wafer
Standard RCA Clean
Dry grow 100nm SiO2
(thermco)
Si
SiO2
Sputter 30nm TiN
TiN
(Not drawn to scale)
AFM Surface Roughness
Compare 3 sputtering tools: Lesker-1 (SNF), Lesker-2 (SNF), AJA (non-SNF)
AFM Step Height
Prometrix Resistivity
XPS/Auger Composition
Measure 3-4x throughout quarter to quantify oxidation over time

## Slide 5: Progress Updates: Fabrication
  RCA clean wafer
  Woollam to measure native oxide thickness (11.2Å)
  Dry oxide growth for 1hr in thermco4 @ 1100℃ (~100nm)
  Woollam to confirm final oxide thickness (~1062.54Å, ~1052.91Å)
    Exact thickness is not important, just there to insulate TiN from Si
    Good quality oxide is important to get accurate TiN surface roughness
  Sputter 30nm TiN (Kapton tape for step)
    AJA (non-SNF)
    Lesker-1 (SNF)
    Lesker-2 (SNF)
  AJA Characterization
    XPS/Auger
    Prometrix
    AFM
  Lesker-1 Characterization
  Lesker-2 Characterization
Lesker TiN target
Si
SiO2
TiN
Update: Lesker-2 expected to go live in early Feb.
Underlined is planned to be done by Friday

## Slide 6: AJA TiN Sputter Recipe: Reactive Sputtering
  Target: Ti
  RF Power: 200W
    150W also ok; different dep rates
  Wafer Bias: 100V
    DC bias 92-94V on AJA in practice
  Ar Flow: 30 sccm
  N Flow: 3 sccm
    Unit conversion means that this is written as 30 on AJA somehow
  Set Pressure: 2.15 mTorr
    1.8-1.9 mTorr on AJA in practice
  Recipe:
  Load sample and wait for 1e-7 base chamber pressure
  Plasma on another target (conductive) e.g. Al, GeTe
    Eases plasma ignition for TiN target
  Plasma on Ti target
    Bias on other target off
  20s ramp-up of Ti target RF power
  2 minutes pre-sputtering of Ti target (shutter closed, no wafer bias)
  20s ramp-up of wafer bias
  Open shutter and deposit for X seconds
  Close shutter
  20s ramp-down of Ti target RF power

## Slide 7: AJA TiN Resistivity and AFM
  Resistivity: Prometrix in SNF
  Sheet resistance: 15.650 Ω/□
  Need step height thickness measurement (to get resistivity and understand AJA deposition rate)
  Step height measurement ran into some issues
  Weird edge artifacts: result of tape permeation?
  Sample has tape residues
  Can clean tape residues and remeasure
    Acetone + IPA + bake
    Any other suggestions?
  Also some areas where chuck blocked sputtering
    Can measure step height and SiO2 roughness
TiN
SiO2 (?)
?
Optical microscope images
?
?
?
TiN
Kapton tape
Residues
SiO2 (?)

## Slide 8: AFM Step Height Measurements

## Slide 9: AFM Roughness Measurements
Roughness: 1.02nm SiO2
Roughness: 1.22nm TiN
0.67nm independent

## Slide 10: AJA XPS Results: Surface Survey Scan

## Slide 11: AJA XPS Results: Hi-Res + Depth Profile

## Slide 12: AJA XPS Results: Fitting
Ti fit has spin-orbit splitting that causes doublet peaks
Ti2p peak has significantly split spin-orbit components (Δmetal=6.1eV).Splitting -value varies with chemical state (Δnitride=6.0eV, Δoxide=5.7eV).
Typically FWHM for each spin-orbit component is the same, but for Ti2p the Ti2p1/2 component is much broader than the Ti2p3/2 peak. Consequently, Ti2p1/2 peak is much shorter than expected.
Caused by Coster-Kronig effect. (Post-ionization, Ti2p1/2 state is very short lived compared to Ti2p3/2 state.)
Causes difficulty in accurately peak fitting Ti2p region with multiple chemical states

## Slide 13: Lesker: Which Recipe? Discussion
  From logbook examination, TiN isn’t used that often in Lesker
  My original plan:
    Master Recipe on Src 2 (TiN source) with downstream control
      35 -> 5 sccm Ar to allow plasma to ignite
      No other sputtering gases
      (How do you adjust N pressure???)
    Didn’t have enough time to run recipe 
  Paul Comita recipe: Ti/TiN co-sputter for higher Ti concentration
  Other recipes call for 3 to 5 sccm Ar with TiN target
  Maybe replicate AJA recipe on Lesker-1?
    XPS shows that it works super well in producing low-oxygen TiN
    May not even need Lesker-2 to do good-quality TiN

## Slide 14: RRAM Process Flow Outline
Si
Si
Pt
SiO2
Start with Si wafer
Standard RCA Clean
Deposit 30nm Pt,
100nm SiO2 (AJA)
Si
Pt
SiO2
Pattern trenches (PT-Ox)
Clean sidewalls of trenches
SiO2
Si
Pt
SiO2
SiO2
HfO2
Deposit 10nm HfO2 (Fiji)
Si
Pt
SiO2
SiO2
HfO2
TiN
Sputter 30nm TiN
Si
Pt
SiO2
SiO2
HfO2
TiN
Pattern top electrodes (PT-MTL)
Clean and deoxidize TiN
Active device area
(Not drawn to scale)

## Slide 15: Process Flow Parameters
  Resistive switching material (metal oxide): hafnia
  Seed layer: none
  Dimensions:
    TiN electrode thickness: 30nm
    Resistive switching layer thickness: 10nm
    Device size: ﻿{1, 2, 3, 4, 5, 8, 10, 20, 40, 50} um
  RS oxide growth temperature: 250C
  Annealing: none
  Metal oxide ALD method: thermal
  TiN deposition method: sputtering
  Top contact: TiN only

## Slide 16: Progress Updates
  RCA clean wafer
  Deposit 10nm Ti with AJA (skipped)
  Deposit 30nm Pt with AJA
  Deposit 100nm SiO2 with AJA
  Woollam to check oxide thickness (834Å)
  Photolithography
    YES Oven for 30 mins
    SVG Coat 2 with 1µm Shipley 3612 resist, 2mm EBR, skip prime step
    Expose with Heidelberg: look at previous runs, logbook, exposure charts by tool (dose: 80, defoc: -2)
    SVG Develop (1µm 3612 dev) w/post-exposure bake and inspect
  PT-Ox: Oxide_ER_Test, 1 min
  Nanospec to check etching
  Matrix for resist ashing: use defaults (Strip.rcp 120s) and inspect to see if resist is removed
  Metal cleaning on wbflexcorr
    SRS-100 for stripping photoresist from metal wafers, 60C
    PRS-1000 for final metal clean before deposition or furnace step, 40C
  Fiji1 thermal HfO2: 100 cycles standard recipe
  Woollam to check oxide thickness
  TiN deposition 30nm
  Photolithography (see previous)
  PT-MTL: still need details
  Microscope to check etching
  Matrix for resist ashing (see previous)
  Metal cleaning on wbflexcorr (see previous)
Underlined is planned to be done by Friday
Notes: Dose: 70, defoc: -2 on Heidelberg-2
Dose: 80ish, defoc: -2 on Heidelberg-1

## Slide 17: Layout Generator

## Slide 18: Layout Generator
Finalized layout: alignment marks, tiling, centering about origin to make Heidelberg usage easier
Design dimensions: about 4cm x 4cm, (20x3 array) x (4x2 grid) devices per size with 10 device sizes
Trench Layer
Top Electrode Layer

## Slide 19: Budget
Item | Type | Time (mins) | Cost ($)
wbclean-1 | Activity | 85 | 70.83
woollam | Activity | 23 | 19.17
woollam | Activity | 12 | 10
Wafer - L-test (100 mm) | Inventory | 4 | 68
svgcoat | Training | 75 | 100
svgdev | Training | 30 | 40
XPS: PHI VersaProbe 3 | Activity | 152 | 126.67
XPS: PHI VersaProbe 3 | Training | 60 | 80
XPS: PHI VersaProbe 3 | Training | 165 | 220
TOTAL |  | 606 | 734.67

## Slide 20: Thank you!
Questions?