## Slide 1: SNF RRAM Standard Process Flow and Characterization of Lesker-2 TiN
Project Members: Akash Levy, Jung-Soo Ko
Staff Mentors: Michelle Rincon, Vijay Narasimhan, J Provine
ENGR241 Winter Project Proposal

## Slide 2: Q2 Motivation
  RRAM is used in lots of research groups at Stanford:
    Simon Wong, Philip Wong, Subhasish Mitra, Jonathan Fan, Yoshio Nishi, etc.
  Difficulties in RRAM processes were shown in a 2015 SNF community service proposal
  Many potential issues there:
    Used very large device sizes in proposal (100um x 100um)
    Patterning devices may cause large sidewall leakage if done naively
    Good quality TiN is required for RRAM
      Required for low resistivity
      Very difficult to do in SNF without oxygen contamination
      ALD tools (Fijis + Savannah) have issues with oxygen leakage
        Previous E241 projects quantified the issue but did not solve it
      Old Lesker takes a very long time to pump down to required level
  Developing a high-quality TiN process on new Lesker would be extremely valuable
  Collecting standard data and creating a standard RRAM process flow would also be very useful for SNF
  SOPs could be easily extended to other types of 2-terminal NVM

## Slide 3: Aim & Goals
  Test and characterize ALD RRAM devices with different parameters
  Create TiN recipe on new Lesker with low oxygen contamination
  Make electrical/imaging data and test structure layouts available to SNF
  Try to solve the problems with RRAM through parameter optimization
  Make SOPs for different RRAM stacks
Process Flow Development
Parameter Optimization
Comprehensive Documentation
SNF Database

## Slide 4: Process Flow Outline
Si
Si
Pt
SiO2
Start with Si wafer
Standard RCA Clean
Deposit 30nm Pt with AJA
Deposit 100nm SiO2 with AJA
Si
Pt
SiO2
Etch trench
Clean sidewalls of trench
SiO2
Si
Pt
SiO2
SiO2
HfO2
Deposit 5nm HfO2 with Fiji
Si
Pt
SiO2
SiO2
HfO2
TiN
Sputter 30nm
TiN with new Lesker
Si
Pt
SiO2
SiO2
HfO2
TiN
Deposit Au with AJA
Pattern top electrodes
Au
Active device area
Not drawn to scale

## Slide 5: Possible Parameters to Optimize
  Resistive switching material (metal oxide): alumina, hafnia, zirconia, tantala, titania
  Alumina seed layer: none, 1nm, 2nm
    Can see if this is necessary early on, ignore if not
  Dimensions:
    TiN thickness: 5nm, 10nm, 20nm, 30nm
    Resistive switching layer thickness: 2nm, 5nm, 8nm, 10nm
    Radius of contact: 50um, 20um, 10um, 5um, 2um, 1um (defined by mask so test all)
  RS oxide growth temperature: 200C, 250C, 300C
  Anneal temperature: none, 300C, 400C
  Plasma vs. thermal
    Theory: thermal ALD will work better since plasma is known to cause interface traps and can also sputter BE metal
  ALD vs. PVD sputtered TiN
    Theory: ALD TiN will not work because of oxygen contamination; new Lesker is better option
  Sputtered TiN
    Optimize: substrate bias, temperature, sputtering gases, etc.
  Top contact: Au, Ag

## Slide 6: Characterization
  All the typical RRAM parameters
    I-V curves for FORM/SET/RESET voltages
    Pulsed-mode tuning
    Endurance, retention
    LRS, HRS, ON/OFF window
  Imaging of TiN on new Lesker
    AFM images for surface roughness
    SEM images
    XPS/Auger composition
  Will use micromanipulator for characterization
  Will use fiji1/2 for ALD resistive-switching (RS) oxide
  Will use AJA for trench SiO2 and all metal deposition
  Will use new Lesker for TiN and Allen 111X AJA for reference in meantime
  How to clean sidewalls? Where to insert cleaning processes?
  Will use 3612 resist and standard photolithography workflow
    yes/svgcoat/Heidelberg/svgdev/PT-Ox|MTL/gasonics
Italicized equipment requires
training

## Slide 7: Tentative Timeline
Week | Description of Activities
1 | Develop process flow, shadow on equipment, do preliminary processing steps (wafer clean, Pt deposition)
2 | Develop layouts, litho training (svgcoat, svgdev, Heidelberg), deposit AJA TiN for comparison Start characterizing AJA TiN (resistivity, composition using XPS/Auger, AFM for surface roughness)
3 | New Lesker training and TiN deposition/characterization (resistivity, compositional analysis, AFM) Finish training and begin processing first sample
4 | Finish processing first sample with AJA TiN, do preliminary electrical characterization Optimize TiN deposition on new Lesker
5 | Process another sample with new Lesker TiN; buffer week
6 | Buffer week to get everything working
7 | Optimize RRAM properties with JUMP and/or test with different materials/layouts
8 | Optimize RRAM properties with JUMP and/or test with different materials/layouts
9 | Optimize RRAM properties with JUMP and/or test with different materials/layouts
10 | Summarize findings, write up SOP, compile data, conclude

## Slide 8: Equipment Usage Budget

## Slide 9: Recap of Deliverables
  SOP on RRAM process flow with optimized layer thicknesses
  Layouts for RRAM test structures
  Optimized TiN recipe on new Lesker sputtering system
  Optimized electrical characterization testbenches
  Electrical characterization data (raw and summarized)
    I-V curves, pulsed mode curves
    Summary of switching characteristics for different device parameters
  All imaging/compositional data (raw and summarized)
    AFM
    SEM
    Auger/XPS

## Slide 10: Updates
  Past week:
    Shadowed on Heidelberg (getting trained on Friday)
    Bought 4-in. Si wafers and RCA cleaned
    Pt bottom contact deposition with AJA
    Finalizing process flow
    Developing layout generator in OpenSCAD
  Upcoming:
    Shadowing/training on SVG tools
    Finishing layouts, finalizing process flow

## Slide 11: Layout Generator

## Slide 12: Thank you!
Questions?